The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles

Specified Requirements of Oil Repellency Textiles

Document No.: FTTS-FA-012

Confidential Level:

Issued Date: August 27, 2004

Revised Date: July 31, 2014

Planning Unit: Specified Requirement Execution Team

Issue Stamp:

| Approved by | Reviewed by | Planning Unit |
| --- | --- | --- |
| Specified Requirement Execution Team |  |  |

The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles

Document Revision History

| Specified Requirements of Oil Repellency Textiles | Document No.: FTTS-FA-012 |
| --- | --- |
| Edition | Revision Reason and Content Description | Revised Page | Revised Date |
| 1.0 2.0 | New issuance Revision according to resolution 2014/07/31 of review committee. |  | 2009/03/27 2014/07/31 |

| Specified Requirements of Oil Repellency Textiles | Document No.: FTTS-FA-012 |
| --- | --- |
|  | Edition: 2.0 |
| Scope: according to the provisions of CNS 11308, Section 1. Definitions: according to the provisions of CNS 11308, Section 2. Grades: as described in Table 1 Oil Repellency Grades. Table 1 Standard Oil Test Oil no. Composition Density (kg/L) Surface tension (25℃) (dynes/cm) Melting point, boiling point (℃) AATCC standard applicable English 0 None --- --- --- 1 Kaydol (naphtha) 0.84-0.87 31.5 348 (boiling point) 2 Kaydol: n-hexadecane (65:35 by volume) 0.82 --- 3 n-hexadecane 0.77 27.3 17~18 (melting point) 4 n-tetradecane 0.76 26.4 4~6 (melting point) 5 n-dodecane 0.75 24.7 -10.5~-9.0 (melting point) 6 n-decane 0.73 23.5 173~175 (boiling point) 7 n-octane 0.70 21.4 124~126 (boiling point) 8 n-heptane 0.69 19.8 98~99 (boiling point) Note: did not pass grade 1 oil tester Test conditions: Test environment: standard temperature and humidity for textile tests is 20±2℃, 65±4% R.H., at least 4 hours. Sampling and preparation: cut at least 3 20 cm x 20 cm sample pieces. Sampling method: sampling should not be conducted at a distance of 1/10 width from selvage; small samples without selvage are an exception, need different vertical and horizontal directions. |
| The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles | Revised Date: 2014/07/31 |
|  | Issued Date: 2004/08/27 |

| Specified Requirements of Oil Repellency Textiles | Document No.: FTTS-FA-012 |
| --- | --- |
|  | Edition: 2.0 |
| Test method: Conducted according to provisions in CNS 11308, Section 8. Ratings: According to provisions in CNS 11308, Section 9. Washing method: According to product standard washing provisions or conditions agreed by interested parties, refer to Table 2. (Only applies to stirring machines with upper-middle openings in CNS 15140). Fill the water to a certain level (18 gal are approximately 68L), adjust water temperature. Add standard cleaner 66±1g (model WOB or same level product), total weight of samples plus wash loading materials is 1.8±0.1kg is placed into the washing machine and washed. Table 2 Washing method Washing cycle Water temperature Drying method Normal/Cotton Sturdy Delicate Durable Press (II) 27±3℃ (III) 41±3℃ (IV) 49±3℃ (V) 60±3℃ (VI) 70±3℃ Hang dry Drip dry Flat dry Flat iron dry Roll dry Normal Durable Delicate |
| The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles | Revised Date: 2014/07/31 |
|  | Issued Date: 2004/08/27 |

| Specified Requirements of Ultraviolet Textiles | Document No.: FTTS-FA-008 |
| --- | --- |
|  | Edition: 3.0 |
| Mark: Washing condition Grade Type Status After washing 10 times Reference purposes I Over 5 Over 3 Durable oil repellent textile II Over 5 --- General oil repellent textile Reference standard: CNS 11038 L 3217-2012 Oil Repellency test method for textiles AATCC 118-2013 Oil Repellency: Hydrocarbon Resistance Test CNS 15140 L3263-2007 Family washing and drying procedures of textiles testing ISO 14419-2012 Textiles – Oil repellency-Hydrocarbon resistance test Supplementary: This standard has been reviewed by the leader of the Specified Requirement Execution Team, and is to be issued after being approved by the chairman of the review committee, same for all revisions. |
| The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles | Revised Date: 2014/07/31 |
|  | Issued Date: 2004/08/27 |