The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles

Specified Requirements of Cycling Clothing

Document No.: FTTS-GA-024

Confidential Level:

Issued Date: December 24, 2013

Revised Date: December 24, 2013

Planning Unit: Specified Requirement Execution Team

Issue Stamp:

| Planning Unit | Reviewed by | Approved by |
| --- | --- | --- |
| Specified Requirement Execution Team | Wen-Hao Xing | Neng-Zhong Lin |

The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles

Document Revision History

| Specified Requirements of Cycling Clothing | Document No.: FTTS-GA-024 |
| --- | --- |
| Edition | Revision Reason and Content Description | Revised Page | Revised Date |
| 1.0 | New issuance |  | December 24, 2013 |

| Specified Requirements of Cycling Clothing | Document No.: FTTS-GA-024 |
| --- | --- |
|  | Edition: 1.0 |
| 1. Applicable Scope: This Standard applies for assessment and test method of basic quality and functional requirement for cycling clothing (see appendix). 2. Grade Standard: 2.1 Basic quality requirements Table 1. Basic quality requirements No. Item Grade 1 Wash durability Fade Over grade 4 Pollution 2 Sweat durability Fade Over grade 4 Pollution 3 Light durability Over grade 4 4 Friction durability (except for white) Dry friction Over grade 4 Wet friction Over grade 3~4 5 6 Textile size change (%) Synthesis fiber and hybrid fabric: -5~+2% Others: -8~+3% 7 Hook pilling (applicable to cycling clothing) Over grade 3 8 Pilling (applicable to cycling painting) Over grade 4 9 Seam efficiency (%) Over 80% 10 Moisture diffusion (mm2) Over 900 11 Drying speed (%) Below 35 12 Moisture absorption - drop (sec) Below 2 13 Moisture absorption - core absorption (mm) Over 80 14 Elongation rate (rebound) (%) Note the elongation rate for the textiles with spring fiber over 90. Remark: The functional color like fluorescence, light reflection or special color decided by the interested parties. |
| The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles | Revised Date: |
|  | Issued Date: December 24, 2013 |

| Specified Requirements of Cycling Clothing | Document No.: FTTS-GA-024 |
| --- | --- |
|  | Edition: 1.0 |
| 2.2 Functional Requirements 2.2.1 Requirement for UV protection textile Classified as the current status and wash 20 times. The wash includes (1) wash label, 8B of Table 7, (2) of Table 3 in CNS 15140 or (3) decided by the interested parties. The requirement for UV protection textiles must reach over 40 according to CNS 15001. 2.2.2 Requirement for antibacterial textile Classified as the current status and wash 20 times. The wash includes (1) wash label, 8B of Table 7, (2) of Table 3 in CNS 15140, (3) decided by the interested parties or agent according to (10) of 3.2 in CNS 14945. The antibacterial activity (staphylococcus aureus and streptococcus pneumoniae) must reach over 2.0 according to CNS 20743. 3. Test Method: 3.1 Test method for wash durability: In compliance with A-2 in CNS1494. 3.2 Test method for sweat durability: In compliance with CNS1496. 3.3 Test method for light durability: In compliance with A in CNS 3846. 3.4 Test method for friction durability: In compliance with Type I in CNS1499. 3.5 Test method for textile size change: The samples refer to CNS 13752 to take the maximum size, and in compliance with 8B of Table 7 in CNS 15140 and (2) drying condition of Table 3. 3.6 Test method for hook pilling: In compliance with A in CNS 12475. 3.7 Test method for pilling: In compliance with A in CNS 8040. 3.8 Seam efficiency: The seam efficiency is calculated according to the following formula after the strength is tested in compliance with 6.2 Test method for seam efficiency of CNS 15538 and CNS 8150. Seam efficiency = Strength after seam/Original strength x 100% 3.9 Test of textile moisture diffusion: In compliance with 4.1 to 4.3 of CNS 15659-1. 3.10 Test of textile moisture drying: In compliance with 4.1, 4.2 and 4.4 of CNS 15659-1. 3.11 Test of textile moisture absorption - drop absorption: In compliance with 4.5 of CNS 15659-1. 3.12 Test of textile moisture absorption - core absorption: In compliance with 4.6 of CNS 15659-1. |
| The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles | Revised Date: |
|  | Issued Date: December 24, 2013 |

| Specified Requirements of Cycling Clothing | Document No.: FTTS-GA-024 |
| --- | --- |
|  | Edition: 1.0 |
| 3.13 Test method for elongation rate: In compliance with B Constant weight of 6.15.2 in CNS 5612 and Table 3. 3.14 Test method for UV protection textiles: In compliance with CNS 15001. 3.15 Test method for antibacterial textiles: In compliance with 8.1 absorption method of ISO 20743. 4. Report: 4.1 Grade of basic quality 4.2 Grade of functional requirement 5. References: CNS 15538 Knitted sport clothing CNS 12475 Test method of hook pilling for weaves and knits CNS 8040 Test method of pilling for weaves and knits CNS 15659-1 Assessment of textile moisture absorption - Part 1: Combination test method CNS 13752 Test method for knit: 6.15.2 Constant weight method of elongation rate CNS 15001 Assessment of UV protection textiles ISO 20743 Textile - 8.1 Absorption method for determination of antibacterial activity of textile products CNS 14945 Assessment of general-purpose antibacterial textiles 6. Appendix This Standard is reviewed by the Specified Requirement Execution Team, and issued after approved by the Committee Director. The same procedures are applied when revised. |
| The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles | Revised Date: |
|  | Issued Date: December 24, 2013 |

| Specified Requirements of Cycling Clothing | Document No.: FTTS-GA-024 |
| --- | --- |
|  | Edition: 1.0 |
| Appendix Basic model for cycling clothing The bicycles include mountain bikes, road bicycles, travel bikes and daily bikes. The clothing will depend on the bike you ride. In order to consider the wind resistance, the cycling clothing will fit the body. The clothing materials are based on the flexibility and light weight to further provide moisture absorption, UV protection and antibacterial. The top clothing is designed with the collar, the zipper, the jacket and the pocket on the rear waist; the painting is trimmed in ergonomics, and designed with a mat in a crotch to avoid the friction and vibration. The mat is designed for fitness, comfort and antibacterial. The cuff can be provided with a skid-proof band to avoid skid. The clothing thickness and the sleeve or painting length can be appropriately adjusted by the season. A vest or a jacket (light weight) can be additionally worn to block the wind and water. In order to enhance the riding safety, the cycling clothing is made in the bright color or embossing. Some of light-reflection sticker and embossment can be sewed on it. Other accessories for cycling clothing include the topee, the head scarf, the mask and the gloves. The cycling clothing applicable to this Standard indicates the top clothing and painting which can fit the body. The reference cases of the cycling clothing are as follows: |
| The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles | Revised Date: |
|  | Issued Date: December 24, 2013 |