The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles

Specified Requirements of Jogging Clothing

Document No.: FTTS-GA-025

Confidential Level:

Issued Date: December 24, 2013

Revised Date:

Planning Unit: Specified Requirement Execution Team

Issue Stamp:

| Planning Unit | Reviewed by | Approved by |
| --- | --- | --- |
| Specified Requirement Execution Team | Wen-Hao Xing | Neng-Zhong Lin |

The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles

Document Revision History

| Specified Requirements of Jogging Clothing | Document No.: FTTS-GA-025 |
| --- | --- |
| Edition | Revision Reason and Content Description | Revised Page | Revised Date |
| 1.0 | New issuance |  | December 24, 2013 |

| Specified Requirements of Jogging Clothing | Document No.: FTTS-GA-025 |
| --- | --- |
|  | Edition: 1.0 |
| Applicable Scope: This Standard applies for assessment and test method of basic quality and functional requirement for jogging clothing (see appendix). Grade Standard: 2.1 Basic quality requirements Table 1. Basic quality requirements No. Item Grade 1 Wash durability (1) Fade Over grade 4 Pollution 2 Sweat durability (1) Fade Over grade 4 Pollution 3 Friction durability (1) Dry friction Over grade 4 Wet friction Over grade 3~4 4 Light durability (1) Over grade 4 5 Textile size change (%) Synthesis fiber and hybrid fabric: -5~+2% Others: -8~+3% 6 Seam efficiency (%) Over 80% 7 Diffusion ability (diffusion area, mm2) Over 1500 8 Drying speed (remaining moisture, %) Below 13 9 Moisture absorption- drop (2) (second) Knit Below 2 Weave Below 5 10 Moisture absorption - core absorption (mm) Over 130 Remark (1). The functional color like fluorescence, light reflection or special color decided by the interested parties. Remark (2). Moisture absorption - the drop method is graded by the averaged value of "no special reflection time". |
| The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles | Revised Date: |
|  | Issued Date: December 24, 2013 |

| Specified Requirements of Jogging Clothing | Document No.: FTTS-GA-025 |
| --- | --- |
|  | Edition: 1.0 |
| 2.2 Functional requirements 2.2.1 Textile air-permeability The air-permeability reaches over 180mm/sec under the test area 20cm2 and pressure 100 Pa. 2.2.2 UV protection The UV protection factor (UPF) for textile reaches over 25 according to CNS 15001 after washed 20 times (in compliance with 2.3). 2.2.3 Textile antibacterial The antibacterial activity for textile (staphylococcus aureus and streptococcus pneumoniae) reaches over 2.0 according to CNS 20743 after washed 20 times (method and agent in compliance with 2.3 and 3.2 (10) of CNS 14945). 2.2.4 Test method for moisture conduction Table 2. Grade for textile moisture conduction Upper-layer wet time (sec) Low-layer moisture absorption (%/sec) Low-layer diffusion radius (mm) Low-layer diffusion speed (mm/sec) One-way conduction index (R) Moisture absorption below 5 over 50 over 18 over 3.0 over 400 over 0.60 |
| The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles | Revised Date: |
|  | Issued Date: December 24, 2013 |

| Specified Requirements of Jogging Clothing | Document No.: FTTS-GA-025 |
| --- | --- |
|  | Edition: 1.0 |
| 2.3 Wash Durability Table 3. Wash durability Item General requirement Standard Wash durability Wash 20 times (A) The knits conform to 8B in CNS 15140 Table 7 and (2) liquid wash condition in Table 3. (B) The weaves conform to 6B in CNS 15140 Table 7 and (2) liquid wash condition in Table 3. Remark: The wash durability not only includes wash 20 times, but also can be decided by the interested parties. 3. Test Method: 3.1 Test method for wash durability: In compliance with A-2 of CNS 1494. 3.2 Test method for dirt durability: In compliance with CNS 1496. 3.3 Test method for scratch durability: In compliance with Type I of CNS 1499. 3.4 Test method for light durability: In compliance with method A of CNS 3846. 3.5 Test method for textile size change: In compliance with CNS 13752G and CNS 8038G for the knits and the weaves. 3.6 Seam efficiency: The seam efficiency is calculated according to the following formula after the strength is tested in compliance with 6.2 Test method for seam efficiency of CNS 15538 and 6.2 Breakage method of CNS 8150. Seam efficiency = Strength after seam/Original strength x 100% 3.7 Test of textile moisture diffusion: In compliance with 4.1 to 4.3 of CNS 15659-1. 3.8 Test of textile moisture drying: In compliance with 4.1, 4.2 and 4.4 of CNS 15659-1. 3.9 Test of textile moisture absorption - drop absorption: In compliance with 4.5 of CNS 15659-1. 3.10 Test of textile moisture absorption - core absorption: In compliance with 4.6 of CNS 15659-1. 3.11 Test method for textile air-permeability: In compliance with CNS 5612. 3.12 Assessment of UV protection textiles: In compliance with CNS 15001. |
| The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles | Revised Date: |
|  | Issued Date: December 24, 2013 |

| Specified Requirements of Jogging Clothing | Document No.: FTTS-GA-025 |
| --- | --- |
|  | Edition: 1.0 |
| 3.13 Test method for textile antibacterial: In compliance with 8.1 Absorption method in ISO 20743. 3.14 Test method for moisture conduction: In compliance with 5.4 in CNS 15659-2. 4. Report: 4.1 Grade of basic quality 4.2 Grade of functional requirement 5. References: CNS 15538 Knitted sport clothing CNS 15659-1 Assessment of textile moisture absorption - Part 1: Combination test method CNS 15659-2 Assessment of textile moisture absorption - Part 2: Test method for moisture conduction CNS 5612 Test method for textile air-permeability GB/T 21980 Specified standard of sport clothing and protection utility CNS 15001 Assessment of UV protection textiles ISO 20743 Textile - 8.1 Absorption method for determination of antibacterial activity of textile products CNS 14945 Assessment of general-purpose antibacterial textiles 6. Appendix This Standard is reviewed by the Specified Requirement Execution Team, and issued after approved by the Committee Director. The same procedures are applied when revised. |
| The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles | Revised Date: |
|  | Issued Date: December 24, 2013 |

| Specified Requirements of Jogging Clothing | Document No.: FTTS-GA-025 |
| --- | --- |
|  | Edition: 1.0 |
| Appendix: Basic models for jogging clothing |
| The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles | Revised Date: |
|  | Issued Date: December 24, 2013 |