The Committee for Conformity Assessment of Association and Certification on Functional and Technical Textiles

Test Method of Specified Requirements of

Water-Vapor Permeable and Liquid-Water Impermeable Textiles

Document No. FTTS-FA-005

Degree of Secrecy:

Enactment Date: 2003.08.29

Modified Date: 2012.12.18

Proposal Unit: Accreditation and Certification Committee

Approval Stamp:

| Proposal | Verification | Approcal |
| --- | --- | --- |
| Accreditation and Certification Committee | Convener: Xing, Wen- Hao | Chairman: Lin, Neng-Chung |

The Committee for Conformity Assessment of Association and Certification on Functional and Technical Textiles

Modification History

| Specified Requirements of Water-Vapor Permeable and Liquid-Water Impermeable Textiles | Document No. FTTS-FA-005 |
| --- | --- |
| Version | Reason and Description of Modification | Modified Page | Modified Date |
| 1.0 2.0 3.0 | New Release Unification of Terminology: from well-done to excellent Approved by The Committee for Conformity Assessment of Association and Certification | 1-2 | 2005.03.03 2012.12.18 |

Water-Vapor Permeable and Liquid-Water Impermeable Textiles

Document No. FTTS-FA-005   Version: 3.0

1. Scope

This criterion is applicable to the evaluation and testing of water vapor permeability & water resistance of textiles.

2. Terminology

2.1 Water-vapor resistance, Ret: Resistance of water-vapor textiles. The unit of resistance of water-vapor is m2．Pa/W. which is used to evaluate the “potential” evaporating steam emitting from textile and apparel under stable water-vapor pressure gradient.

.

2.2 Water penetration resistance, Wp: the degree a textile can resist water penetration, used as mmH2O.

3. Qualification and Testing items

3.1 Water-vapor resistance, Ret

Diagram 1 Grades of Water-vapor Resistance

| Items | Grade | Requirement | Classification |
| --- | --- | --- | --- |
| Water-vapor resistance m2．Pa/W | 1 | 40 ≦Ret ＜50 | Fair |
|  | 2 | 27 ≦Ret ＜40 | Moderate |
|  | 3 | 13 ≦Ret ＜27 | Good |
|  | 4 | 6 ≦Ret ＜13 | Very good |
|  | 5 | Ret ＜6 | Excellent |

The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles

Modified Date: 2012.12.18

Released Date: 2003.09.01

3.2  Water Pressure (WP)

Diagram 2 Grades of Water Pressure

| Items | Grade | Requirement | Classification |
| --- | --- | --- | --- |
| Water Pressure mmH2O | 1 | 300≦WP＜2000 | Fair |
|  | 2 | 2000≦WP＜4000 | Moderate |
|  | 3 | 4000≦WP＜8000 | Good |
|  | 4 | 8000≦WP＜15000 | Very Good |
|  | 5 | 15000≦WP | Excellent |

3.3 General requirement

Choose the proper general requirement by each product’s end-use

Diagram 3  General Requirement

| Item | Requirement |
| --- | --- |
| Washing durability | Evaluate the appearance after wash first. No damaged appeared, determine the hydrostatic pressure. Cycles of washing decided by the type of textile |
| Flexing resistance in cold condition | Evaluating the appearance after 20000 cycles flexing |
| Adhesion strength | > 200 g/cm |

The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles

Modified Date: 2012.12.18

Released Date: 2003.09.01

Water-Vapor Permeable and Liquid-Water Impermeable Textiles

Document No. FTTS-FA-005   Version: 3.0

4. Test method

4.1 Water-vapor resistance

The test performed in accordance with CNS 15102 L3256 procedure 6.4.

4.2 Water resistance

The test performed in accordance with CNS 10460 L3201 A2.

4.3 Home laundering

In accordance with CNS 15140 L3263, textiles are washed by tumble washer and dry flat; adopting 6A washing procedure and hang dry in accordance with 6A dry procedure; or 7B wash procedure and tumble dry in accordance with E dry procedure with 50℃.

4.4 Flexing resistance in a cold condition

Refer to ISO 7854 method C, cut specimens in size of 22cm×19cm with longer dimension paralleling to the longitudinal and transverse direction of the material respectively.  Each test piece shall be sewn into a cylindrical shape 19cm long × 6.4cm inside diameter.  Condition the specimens in the -20℃ for 24 hours, mount the cylindrical test piece between the two discs.  One disc shall be capable of moving at 152 compression strokes per minute; the second disc shall be at the speed of 200 twist insertions per minute.  Set the apparatus in motion and stop it after specified number of flexes, assess the flexing damage.

4.5 Adhesive strength

Refer to ISO 2411, take five test specimens cut with the length parallel to the longitudinal and transverse direction respectively.  Separate the layers of test specimen 5cm along with its longer dimension.  Clamp each side by the jaw of the tensile strength testing machine, separating the layer of specimen in the specified speed to determine the adhesive strength.  Where the layer is not sufficiently strong to be stripped, choose the seal of HIPSTER, model no. HP168 or other correspondent with the good adhesive property, bonded with the layer of test specimen by heat to determine the adhesive strength accordingly.  When the three-layered material is tested, each combination shall be tested respectively and choose the lower adhesive strength in bonding to be reported.

The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles

Modified Date: 2012.12.18

Released Date: 2003.09.01

Water-Vapor Permeable and Liquid-Water Impermeable Textiles

Document No. FTTS-FA-005   Version: 3.0

5. Signs

| Type | Water-vapor resistance | Water resistance | Water resistance (wash pre-processing) | Flexing resistance in cold condition | Adhesion resistance | Application |
| --- | --- | --- | --- | --- | --- | --- |
| I | >4 | > 4 | 10 times wash >4 | No change in appearance | ＞ 200g/cm | harsh climate |
| II | >2 | > 5 | 10 times wash >4 | No change in appearance | ＞ 200g/cm | fishing |
| III | >3 | > 3 | 5 times wash >3 | No change in appearance | ＞ 200g/cm | Mountain climbing and skiing |
| IV | >2 | > 4 | 10 times wash >2 | No change in appearance | ＞ 200g/cm | Breathable raincoat |
| V | >4 | > 2 | 5 times wash >2 |  | ＞ 200g/cm | Breathable raincoat, jacket, etc. |
| VI | >2 | > 3 | 5 times wash >2 |  | ＞ 200g/cm | Windproof windbreaker, jacket, etc. |
| VII | >2 | > 2 | 5 times wash >1 | No change in appearance | ＞ 200g/cm | Ordinary windbreaker, jacket, etc. |

6. Standard:

6.1 CNS 15000 L1034  Evaluation of waterproof breathable textiles

6.2 CNS 15102 L3256  Comfort of textiles- measurement of thermal resistance and water-vapor resistance (sweating-guarded hotplate test) under stable conditions

6.3 CNS 10460 L3201 Measurement of waterproof resistance on fabric product --- water resistance

6.4 CNS 15140 L3263 Measurement of textiles of home laundry and drying procedure

6.5 ISO 7854       Rubber- or plastics-coated fabrics—Determination of resistance to damage by flexing

6.6 ISO 2411           Rubber- or plastic-coated fabrics—Determination of coating adhesion

7. Appendix:

The standard is audited by Accreditation and Certification committee, submitted to, approved of, and released by Accreditation Committee, the same as modification.

The Committee for Conformity Assessment of Accreditation and Certification on Functional and Technical Textiles

Modified date: 2012.12.18

Release date: 2003. 09.01